THERMAL INSULATION

SECTION 07 21 19

Foamed-in-Place Insulation

HEATLOK SOYA HP

This specification utilizes the Construction Specifications Institute’s (CSI) and CSC 3-Part formatting.  The specification is a manufacturer-specific product specification to be used by design professionals as a guide specification.  Editing notes are indicated in red italics and for D-Max projects in blue and precede specification text.  Delete editing notes in final specification.

This specification specifies medium density spray foam insulation by Huntsman Building Solutions.  Revise section number and title below to suit project requirements.

The specified product may contribute to the following credits/points for the respective rating system:

LEED V.4.1

.

## PART 1 – GENERAL

1.1.	GENERAL

- Conform to sections of Division 01 xx xx as applicable.

1.2.	WORK INCLUDED

- Spray application of polyurethane foam to provide insulation, air barrier and vapour barrier, including surface preparation.

1.3.	INCLUDED SECTIONS	Note: Optional Amend to suit project

Supply and installation of transition strip membrane, through wall flashing and primer material as required in accordance with sections 07 25 00 and 07 27 00.

1.4.	RELATED SECTIONS	Note: Amend to suit project

- Concrete Curing 								Section 03 39 00

- Structural Pre-cast Concrete					Section 03 40 00

- Unit Masonry									Section 04 05 00

- Metal Decking									Section 05 10 00

- Rough Carpentry								Section 06 10 00

- Waterproofing									Section 07 10 00

- Vapour Barrier									Section 07 26 00

- Air Barrier Section								Section 07 27 00

- Flexible Flashing								Section 07 65 00

- Pre-formed Roofing and Cladding/Siding		Section 07 70 00

- Fireproofing									Section 07 80 00

- Thermal Barrier								Section 07 81 29

- Fire Block										Section 07 84 00

- Gypsum Board								Section 09 20 00

1.5.	REFERENCES

- CAN/ULC-S705.1-18 Standard for Thermal Insulation Spray Applied Rigid Polyurethane Foam, Medium Density, Material Specification.

- CAN/ULC-S705.2 Standard for Thermal Insulation Spray Applied Rigid Polyurethane Foam, Medium Density, - Application.

- CALIBER Quality Assurance Program.

- CCMC 14505-L Spray Polyurethane Foam Insulation HEATLOK SOYA HP

- CAN/ULC-S770-09 Standard Test Method For Determination Of Long-Term Thermal Resistance of Closed-Cell Thermal Insulating Foams.

- Greenguard Gold Certification – Interior Air Quality

- ISO/TS 11665-13 (method C K124/02/95) Measurement of radioactivity in the environment - Air: radon-222 -- Part 13:Determination of diffusion coefficient in waterproof materials using activity concentration measurement.

1.6.	SUBMITTALS AND SAMPLES

- Before starting the work, submit in accordance with sections 01 33 00, result of independent laboratory test reports, data sheets, physical proprieties, meeting or exceeding requirements of the standard in reference to this specification.

- Submit a laboratory report of the adhesion compatibility with: flashing membranes, coatings and substrates.

- License under CALIBER and certification of applicators under CALIBER to be submitted to the consultant upon request and prior to the beginning of the work.

- Submit by the manufacturer a conformity certification to NBC of the polyurethane foam system.

- Submit test results by an independent and SCC certified laboratory on air barrier material performance, conducted in order to certify that the air barrier material rating meets National Building Code requirements and this specifications art: 2.3.11.

- Submit test results by independent laboratory on LTTR values according to CAN/ULC-S770 for all SPF system used on the project. Other test methods will not be accepted.

1.7.	QUALITY ASSURANCE

- Contractor performing work under this section must be certified by CALIBER or have a experience of a minimum of 5 years.

- Upon request of consultant, submit a copy of the contractor quality control report as requested in CAN/ULC-S705.2.

- Conduct site tests of sprayed work as required by the CALIBER Quality Assurance Program.

- Upon request, submit manufacturer/supplier field applied product quality control report. For D-Max projects, this can be completed for each floor.

- Schedule a start-up meeting to reviews details and coordinate sequencing with different professionals and the spray foam applicator.

1.8.	MOCK-UP

- Provide mock-up of insulation and air barrier in accordance with section 01 75 00.

- Construct typical exterior sample wall in conjunction with section 01 75 00, incorporating window frame head jamb and sill and building corner condition with foundation wall junction.

- Acceptance of mock-up sample may be part of the completed work.

- Do not commence work until sample installation has been accepted.

- Acceptance of sample preparation will be a reference for minimum acceptance of the work. Any need for deviation of the mock-up acceptance shall be reported in writing.

- Upon consultant request, provide in writing manufacturer acceptance of the mock-up quality.

1.9.	DELIVERY, STORAGE AND HANDLING

- Materials shall be delivered in manufacturers original sealed containers clearly labelled with manufacturer’s name, product identification, safety information, net weight of contents, and expiring date.

- Material is to be stored in a safe manner and where the temperatures are in the limits specified by the material manufacturer.

- Empty containers have to be removed from site on a daily basis in accordance with

CAN/ULC-S705.2.

1.10.	WARRANTY

- Warrant work of this section against defects and deficiencies for a period of two years from date work completion.

- Provide manufacturer’s warranty for the field-applied product.

PART 2 - PRODUCTS

## ENVIRONNEMENTAL REQUIREMENTS

- The product shall not contain any CFC, HCFC, HFC or any ozone depletion substance.

- The Spray Polyurethane Foam Insulation shall have a minimum of 18 % recycled content from post-consumer and post-industrial sources. The % shall be calculated by weight basis ratio of the recycled source in the final SPF system to be applied on the building.

- The SPF shall contain a minimum of 4 % renewable content.

- The product shall have a HFO blowing agent with a global warming potential of maximum 1. (GWP)

- Product shall conform to GREENGUARD Gold certification.

## MATERIALS

- Spray Applied Polyurethane Foam Insulation system in accordance with CAN/ULC S705.1-15 Standard for Thermal Insulation Spray Applied Rigid Polyurethane Foam, Medium Density, Material Specification and those specific objectives performances.

- Product:  HEATLOK SOYA HP

- The product shall be evaluated by the CCMC.

## PHYSICAL PROPERTIES

| Density | ASTM D1622 | 2.20 lb/ft3 | 35.32 Kg/m³ |
| --- | --- | --- | --- |
| Long Term Thermal Resistance (LTTR) Design value | CAN/ULC S770 -09 CAN/ULC S705.1-15 | 100 mm / R-26 75 mm / R-18 50 mm / R-12 | 100 mm / 4.50 RSI 75 mm / 3.25 RSI 50 mm / 2.06 RSI |
| Dimensional stability | ASTM D-2126 (% of change in volume at 28 days) -20°C 70°C H.R. ˃ 97 +/- 3% 80°C | +0.2 % +7.3 % +2.7 % |
| Flame Spread Index | CAN/ULC S102-S127 | 300 |
| Compressive strength | ASTM D1621 | 37 lb/in2 | 253 KPa |
| Tensile strength | ASTM D1623 | 69 lb/in2 | 475 KPa |
| Open cells | ASTM D6226 | 3 % |
| Water absorption | ASTM D2842 | 2 % |
| Air Permeance | ASTM E 2178-13 (25 mm, top skin removed) | 0.0051L/s· m²@75 Pa |
| Fungi Resistance | ASTM C1338 | No Fungal Growth |
| VOC | CAN/ULC S774 | 1 day |
| VOC | GREENGUARD Certification | Gold |
| Water vapour permeance | ASTM E96 (50 mm) | 0.55 perm | 31 ng/Pa s.m² |
| Radon Diffusion Coefficient | ISO/TS 11665-13 (method C K124/02/95) | <(2,5±0,3).10-11 m2/s |
| Radon Resistance Coefficient 50mm | ISO/TS 11665-13 (method C K124/02/95) | <237 910.106 s/m |
| Building Face Protection | Article 3.2.3.8. NBC 2015 | In Progress |

  - PRIMERS

- Install primers in accordance with the manufacturer recommendations and the CAN / ULC-S705.2 standard.

- For oily metal surface like Z-Bar, steel deck roof or curtain wall pan, aluminum tube, and PVC, before spraying polyurethane foam apply ADBOND 8388-1 adhesive primer, color: red.

2.5		EQUIPMENT

Equipment shall be as recommended in CAN/ULC-S705.2 and approved by the foam manufacturer for type of application.

PART 3 – EXECUTION

Note: Check the adhesion and compatibility for: flashing, membranes, coatings, and follow HUNTSMAN BUILDING SOLUTIONS typical details drawing.

3.1 	EXAMINATION

- Verify that surfaces and conditions are suitable to accept work as outlined in this section. At the consultant request, an inspection will be completed by HUNTSMAN BUILDING SOLUTIONS to confirm the work is acceptable prior to the foam installation.

- According to the prescriptions of the standard CAN/ULC-S705.2, verify the conditions of surfaces.

- Surfaces to be covered with spray foam shall be free of an excess of moisture, frost, oil, rust, and any other foreign material able to have a negative effect on the adhesion of the product. In doubt, apply a primer.

- Allow time for the complete cure of the substrates: concrete, mortar, fillers, membranes, primers, coatings or other surfaces, before applying the spray foam.

- Verify the adhesion of membranes and coatings to different substrates are good, taking in account the climatic conditions for the application of membranes, coatings and spray foam.

- If the thickness of application is 50 mm or greater, the membrane detail around opening must be installed in accordance with HUNTSMAN BUILDING SOLUTIONS typical details. Drawings are available at www.huntsmanbuildingsolutions.com or contact your representative. Option, use mechanical fastener to secure self-adhesive membranes around openings only.

- Option 1, use mechanical fastener to secure self-adhesive membranes around openings or where the spray foam stops directly on a membrane. (galvanized steel angle: 13 mm x 25 mm x 0.42 mm in thickness (gypsum corner bead). Fixed at 400 mm C/C).

Note: Refer to mechanical fastener section (07 27 00) for coordination.

b) Option 2, no mechanical fastening, premembraned plywood (see Huntsman Building Solutions typical details)

- All oily metal surface like Z-Bar, steel deck roof or curtain wall pan, aluminium tube, and PVC, shall be primed as referenced in CAN / ULC S705.2 art: A 1.7.

If required, all spray applied membrane shall be installed before “Z” bars.

- Identify the moisture content of all different building materials.

- Report in writing any defects in surface or conditions that may adversely affect the performance of products installed and follow manufacturer’s recommendations.

- For occupied building application, confirm that all requirements in Article 1.11 are in place.

- Commencement of work outlined in this section shall be deemed as acceptance of existing work and conditions.

- Ensure that all the work that needs to performed prior to the application of the spray foam insulation is completed. Including these elements, but without limitation:

- Masonry anchor;

- Furring, wood blocking, sub-frames, flashing, mechanical fastening;

- Coatings, membranes, flashings, mechanical fastening

- Mechanical and electrical works;

- Fire-stop

- Primer.

3.2	APPLICATION

- Spray application of polyurethane foam shall be performed in accordance with CAN/ULC-S705.2.

- Apply spray foam on dry, solid and clean surfaces when the climatic conditions are in accordance with the CAN/ULC S705.2 standard and with Huntsman Building Solutions recommendations.

- Apply only when surfaces and environmental conditions are above -20oC (-4oF). Refer to technical data sheets.

- Apply in consecutive passes (min. 15 mm (5/8’’), max. 50 mm (2’’))

- Apply to obtain the thickness as indicated on drawings, or (   mm) for wall, (   mm)  for roof to achieve the required thermal insulation value. Use only the Long Term Thermal Resistance (LTTR) CAN/ULC S 770 test method to calculated design R value.

- Do not spray closer than 3” (75 mm) to chimneys, recess spotlight or other source of heat.

3.3	TOLERANCE

- Apply the product to achieve an average thickness of ± 6 mm (1/4”), from (9 readings on 1 m2), of the thickness requirements in the drawings at a minimum of 1 m2 readings for each 150 m2 surface sprayed.

- Apply the insulation uniform in accordance to NBC article 9.25.2.3. 1).

3.4       APPLICATION CONDITIONS

- At the beginning and during the work, allow access to the job site by HUNTSMAN BUILDING SOLUTIONS representatives.

- Execute the work of this section when the temperature of the air and substrate are within the limits of the data sheet supplied by the manufacturer.

- Apply the spray foam only when the relative humidity is below 80%.

- Prepare all surfaces in accordance with the manufacturer’s recommendations and CAN/ULC-S705.2 Standard.

3.5 	 PROTECTION

- Ventilate area receiving insulation to maintain safe working conditions.

- Ensure the safety of the workers in conformity with local regulations, standards and manufacturers recommendations.

- For spraying inside of occupied buildings:

- Delimit the working space (with a polyethylene if required).

- All the ventilation ducts must be sealed before the spraying.

- Install a fan extracting air outside the building.

- The workspace, in retrofit construction (occupied buildings), must be under negative pressure at a minimum exfiltration rate of 0.3 air changes per hour.

- The workspace, in retrofit construction, must be under negative pressure for a minimum of 24 hrs.

- Confirm everyone in the workspace has respiratory protective equipment and personal protective equipment in conformity with provincial regulations and the CAN/ULC-S705.2 standard.

- Protect adjacent surfaces, windows, equipment, and site areas from damage of over spray.

3.6	QUALITY CONTROL ON SITE

If requested, a quality control report will be issued after a site inspection by Huntsman Building Solutions.

3.7 	FIRE PROTECTION

- Any open flame or welding is not permitted to be in contact with the Spray Polyurethane Foam in place. Use protection as required in CAN / ULC S705.2.

- All plastic insulation must be protected from interior occupancy space by an approved thermal barrier to meet the requirements of local Building Codes.

Note: Work related to thermal barrier installation should be specified under appropriate sections.

END OF SECTION 07 21 19